## Slide 1: Guidelines for Selecting Sign Sheeting Materials for AASHTO M268
PI: Gene Hawkins, Ph.D., P.E.
Texas A&M University,
Texas A&M Transportation Institute
NCHRP Project No. 20-07/Task 374

## Slide 2: Retroreflective Sign Sheeting
Redirects light from headlight back toward vehicle
Retroreflective sign sheeting makes signs more visible at night
  Especially at a distance
Many factors affect sign brightness
Range of choices for sign sheeting
  Challenge is selecting an appropriate sheeting for a given application

## Slide 3: Project Objective
Develop guidance for agencies to select sign sheeting materials using AASHTO M268 specification
Project was a limited resource project
  Not able to address all factors affecting sheeting selection

## Slide 4: AASHTO Sheeting Spec
M268: Standard Specification for Retroreflective Sheeting for Traffic Control
  Revised 2015 to provide 4 sheeting types
AASHTO sheeting types:
  A: encapsulated bead
  B: microprismatic without significant 1 observation angle performance
  C: microprismatic with significant 1 observation angle performance
    No products currently certified as Type C
  D: microprismatic with 0.5 & 1 observation angle performance about twice that of Type C

## Slide 5: Project Activities
Measure selection of sheeting materials
  Create generic AASHTO sheeting types
Create selected roadway and sign scenarios (15 individual scenarios)
Calculate luminance supplied by generic sheeting types
Compare to luminance demand
Develop general guidelines

## Slide 6: Sheeting Evaluation
Calculate luminance for specific conditions (supply luminance)
  Roadway size and alignment, vehicle size, headlamps, sign position, sheeting
  Used ERGO program
  Required measuring sheeting retroreflectivity
Determine demand luminance
  Used research by others
  Based on sign legend size and driver accommodation level
Compare supply and demand luminance

## Slide 7: Sign Luminance
Sign luminance: apparent brightness
Function of:
  Headlamp performance
  Sheeting retroreflectivity
  Viewing geometry
To evaluate, need sheeting retroreflectivity (RA) for each combination of four viewing angles:
  Observation, entrance, rotation, orientation

## Slide 8: RA Measurement Angles
: observation
: entrance
: rotation
: orientation

## Slide 9: Supply Luminance Calculations
Used ERGO
  Developed by Avery-Dennison
  No longer available
Inputs
  Roadway alignment
  Vehicle size
  Headlamp performance
  Sign position
  Sign sheeting retroreflective performance

## Slide 10: Sheeting RA Measurement
Measured in lab
  ERGO prismatic files have > 500K points
  Too many for this project
Determine min number of measurement points (1,750 used for project)
  Retroreflectivity array size limited by lab equipment
  Array size prevented analysis of some roadway scenarios (short radius curves, left side signs)
Measured 5 products (11 samples total)

## Slide 11: Sample Measurement
All samples were white sheeting
Sample measurement:
  Type A
    Single product, average of 2 samples
  Type B
    Average of 2 products, each product is average of 2 samples
  Type C
    Not measured, no current product
    Created “pseudo-Type C” from ERGO retroreflectivity file
  Type D
    Two products, each product is average of 2 or 3 samples
Average sample measurements averaged to create generic RA file for each sheeting type
Yellow and orange sheeting
  Created by applying M268 color correct factors to all 1750 measurements
    Used standard yellow for yellow (0.75white)
    Used fluorescent orange for orange (0.30 white)

## Slide 12: Pseudo Type C Sheeting
For supply luminance analysis, use single material included in the original release of ERGO
  ERGO retroreflectivity measurements are not representative of the current version of the product on the market
  Product (old or new) does not meet Type C specification
Type C material not included in guidelines

## Slide 13: Roadway Alignment
Calculated supply luminance for:
  Straight road
  Curved road (left and right)
    643 ft radius (represents 45 mph speed)
    1,333 ft radius (represents 60 mph speed)
Retroreflectivity measurement limitations prevented analysis of 30 mph curve (231 ft radius)

## Slide 14: Vehicle Size
Supply luminance associated with best selling light pickup truck
  2018 model year
  Driver height: 5 ft, 6 in
Basis for light pickup:
  Best selling vehicle model in US
  Larger vehicle produces lower luminance than for typical sedan

## Slide 15: Headlamp Performance
Headlamp performance used UMTRI 2019 data for 2018 model year headlamps
  LED and tungsten-halogen headlamps
  25th, 50th, and 75th market-weighted percentile performance
  Array: ±25º horz, +7º to -5º vert
Used 50th percentile LED headlamp to calculate supply luminance

## Slide 16: Sign Placement
Post-mounted
  Right side of 2-lane and 4-lane roads
  Sign centroid: 14 ft offset, 9 ft high
Overhead
  Centered over lane to left of vehicle
  Centroid: 22 ft above road

## Slide 17: Demand Luminance
Two conditions based on scene complexity
  Low/Medium/High with Lighting
    Represents rural, suburban, lit urban
  High without lighting
    Represents urban without street lights
Older driver accommodation
  Plots for 50th, 75th, 85, and 95th percentile accommodation
Data from CIE report
  Based on legibility index applied to LOOK3 model
  Legibility index multiplied by sign letter height provides limits of LOOK3 range

## Slide 18: LOOK3 Model

## Slide 19: Roadway & Signing Scenarios
Roadway scenarios (5 total)
  Tangent
  Curved: left and right, 643 and 1,333 ft radii
Sign placement
  2-lane: centroid 14 ft from edge line, 9 ft above edge line
  4-lane: centroid 14 ft from edge line, 9 ft above edge line, vehicle in left lane
  Freeway: overhead sign centered above lane to left of vehicle, centroid 22 ft above pavement
Sign scenarios
  White: 16- (overhead), 10-, and 6-inch legends
  Yellow: 6-inch legend
  Orange: 5-inch legend

## Slide 20: Comparing Supply/Demand
Many plots prepared comparing supply and demand luminance
  45 plots each for two types of scene complexity
Plots provide supply luminance for:
  Sheeting types
  Roadway alignment
Plots provide demand luminance for:
  Percent accommodation
  Scene complexity
  Sign letter height

## Slide 21: Sample Plot
4-lane, post-mounted white sign (6 in legend), curve right (643 ft R), high complexity without lighting

## Slide 22: Study Limitations
Complicated topic, not feasible to simplify
  Many variables affect results
RA files:
  Type C not included in guidelines
  Size limited ability to evaluate wide range of conditions
  Does not include all materials that meet AASHTO specification
  May not have adequate number of samples of each product
  Yellow and orange data may not be accurate
  RA values do not represent the manufacturers minimum performance or the minimum performance of ASTM or AASHTO sheeting types
Results represent new material
  RA performance of aged sheeting not known

## Slide 23: Luminance Variability
Recent TRR paper evaluated variability in luminance as function of input variables
Headlamp example (straight road, 6-in legend):
116 cd/m2
452%

## Slide 24: Guideline Summary: L/M/Hw
Scene complexity: low, medium, high with lighting
Type A:
  Mostly provides 75% accommodation on 2-lane roads
  Multilane: use only with large legend
  Not recommended with yellow/orange signs
  Overhead provides 75% accommodation on tangent alignment (limit use to tangent only)
Type B:
  White large legend mostly provides 95% accommodation
  White (small legend) and yellow mostly provides 75% accommodation
  Not recommended for orange signs
  Overhead: mostly 95% accommodation on tangent, mostly 75% accommodation on curved
Type C: not addressed
Type D:
  Mostly provides 85-95% accommodation for white and yellow
  Mostly provides 50% accommodation for orange
  Preferred type for overhead
Report provides additional details for guidelines

## Slide 25: Guideline Summary: Hwo
Scene complexity: high without lighting
Type A:
  Not recommended
Type B:
  50-85% accommodation on 2- & 4-lane roads depending upon scenario
  Not recommended for orange and overhead signs
Type C: not addressed
Type D:
  Mostly provides 50-85% accommodation for white and yellow
  Generally provides 50% accommodation for orange
  Preferred for overhead signs
Report provides additional details for guidelines

## Slide 26: Recommendations
Create pubic domain luminance calculation tool
Manufactures and agencies should work to develop fully characterized retroreflectivity files for sheeting products used by agencies
Refine research on demand luminance
Create fully characterized retroreflectivity files for sheeting near end of service life
Evaluate luminance for a wider ranges of vehicle sizes, headlamps, and roadway geometry
Revise Type C RA values in M268 so that some products will meet Type C spec
  Set 0.2°/-4° geometry between 350-450 cd/lux/m2