Appendix C

HWTD Data and Graphs

Figure C - 1.  HWTD Results – SGC Specimens – Georgia Granite Mix.

Figure C - 2.  HWTD Results – SGC Specimens – Arkansas Gravel Mix.

.

Figure C - 3.  HWTD Results – SGC Specimens – Wisconsin Gravel Mix.

Figure C - 4.  HWTD Results – SGC Specimens Mississippi Chert  Mix.

Figure C - 5.  HWTD Results – SGC Specimens – Kentucky Limestone Mix.

Figure C - 6.  HWTD Results – SGC Specimens – Oklahoma Sandstone  Mix.

Figure C - 7.  HWTD Results – SGC Specimens – Pennsylvania Dolomite  Mix.

Figure C - 8.  HWTD Results – SGC Specimens – Wyoming Gravel  Mix.

Table C - 1.  Results of HWTD Tests on Georgia Granite Mix at 50˚C

|  | Track |
| --- | --- |
|  | Left | Right |
|  | ID | Air Void, % | ID | Air Void, % |
|  | MD 307.09 | 7.4 | MD 307.11 | 7.3 |
|  | MD307.10 | 7.3 | MD 307.12 | 7.7 |
| Rut Depth at 6960 passes, mm | 12.5 | NA |
| Rut Depth at 8960 passes, mm | NA | 12.5 |
| Creep Slope, Passes/mm | 1354 | 2030 |
| Strip Slope, Passes/mm | 383 | 571 |
| Stripping Inflection Point, Passes | 4661 | 5661 |

Table C - 2.  Results of HWTD Tests on Arkansas Gravel Mix at 50 ˚C

|  | Track |
| --- | --- |
|  | Left | Right |
|  | ID | Air Void, % | ID | Air Void, % |
|  | MD 311.0.9 | 7.0 | MD 311.11 | 6.8 |
|  | MD311.10 | 7.0 | MD 311.12 | 6.8 |
| Rut Depth at 10,000 passes, mm | 8.5 | 7.4 |
| Rut Depth at 20,000 passes, mm | 11.1 | 9.0 |
| Creep Slope, Passes/mm | 3,600 | 5,320 |
| Strip Slope, Passes/mm | NA | NA |
| Stripping Inflection Point, Passes | NA | NA |

Table C - 3.  Results of HWTD on Wisconsin Gravel Mix at 50 ˚C

|  | Track |
| --- | --- |
| Binder | PG 58-28 |
|  | Left | Right |
|  | ID | Air Void, % | ID | Air Void, % |
|  | MD 313.09 | 6.6 | MD 313.11 | 6.7 |
|  | MD 313.10 | 6.7 | MD 313.12 | 6.7 |
| Rut Depth at 2,860 passes, mm | 12.5 | 12.5 |
| Rut Depth at 10,000 passes, mm | NA | NA |
| Rut Depth at 15,000 passes, mm | NA | NA |
| Rut Depth at 20,000 passes, mm | NA | NA |
| Creep Slope, Passes/mm | NA | NA |
| Strip Slope, Passes/mm | NA | NA |
| Stripping Inflection Point, Passes | NA | NA |

Table C - 4.  Results of HWTD Tests on Mississippi Chert Mix at 50 ˚C

|  | Track |
| --- | --- |
| Binder | PG 64-22 |
|  | Left | Right |
|  | ID | Air Void, % | ID | Air Void, % |
|  | MD 314.09 | 6.9 | MD 314.11 | 7.0 |
|  | MD 314.10 | 6.9 | MD 314.12 | 7.0 |
| Rut Depth at 2,860 passes, mm | 4.1 | 4.0 |
| Rut Depth at 10,000 passes, mm | 5.8 | 5.6 |
| Rut Depth at 15,000 passes, mm | 6.4 | 6.1 |
| Rut Depth at 20,000 passes, mm | 7.0 | 6.6 |
| Creep Slope, Passes/mm | 6550 | 8074 |
| Strip Slope, Passes/mm | NA | NA |
| Stripping Inflection Point | NA | NA |

Table C - 5.  Results of HWTD on Kentucky Limestone Mix at 50 ˚C

|  | Track |
| --- | --- |
| Binder | PG 64-22 |
|  | Left | Right |
|  | ID | Air Void, % | ID | Air Void, % |
|  | MD 315.09 | 6.4 | MD 315.11 | 6.4 |
|  | MD 315.10 | 6.3 | MD 315.12 | 6.3 |
| Rut Depth at 7,100 passes, mm | NA | 12.5 |
| Rut Depth at 8,000 passes, mm | 12.5 | NA |
| Rut Depth at 10,000 passes, mm | NA | NA |
| Rut Depth at 15,000 passes, mm | NA | NA |
| Rut Depth at 20,000 passes, mm | NA | NA |
| Creep Slope, Passes/mm | 1,364 | 1,273 |
| Strip Slope, Passes/mm | 500 | 500 |
| Stripping Inflection Point | 6,200 | 5,051 |

Table C - 6.  Results of HWTD on SGC Specimens for Oklahoma Mix at 50 ˚C

|  | Track |
| --- | --- |
| Binder | PG 76-22 |
|  | Left | Right |
|  | ID | Air Void, % | ID | Air Void, % |
|  | MD 316.03 | 7.0 | MD 316.05 | 6.3 |
|  | MD 316.04 | 6.3 | MD 316.06 | 6.6 |
| Rut Depth at 10,000 passes, mm | 2.4 | 1.5 |
| Rut Depth at 15,000 passes, mm | 2.5 | 1.6 |
| Rut Depth at 20,000 passes, mm | 2.7 | 1.8 |
| Creep Slope, Passes/mm | 36,750 | 61,500 |
| Strip Slope, Passes/mm | NA | NA |
| Stripping Inflection Point | NA | NA |

Table C - 7.  Results of HWTD Tests on Pennsylvania Dolomite Mix at 50 ˚C

|  | Track |
| --- | --- |
| Binder | PG 64-22 |
|  | Left | Right |
|  | ID | Air Void, % | ID | Air Void, % |
|  | MD 317.03 | 6.6 | MD 317.05 | 6.2 |
|  | MD 317.04 | 6.4 | MD 317.06 | 7.0 |
| Rut Depth at 10,000 passes, mm | 8.9 | 8.6 |
| Rut Depth at 15,000 passes, mm | 10.1 | 10.4 |
| Rut Depth at 20,000 passes, mm | 11.7 | 12.5 |
| Creep Slope, Passes/mm | 4,895 | 2,486 |
| Strip Slope, Passes/mm | 2,830 | 1724 |
| Stripping Inflection Point | 14,800 | 14,600 |

Table C - 8.  Results of HWTD Tests on Wyoming Gravel Mix at 50 ˚C

|  | Track |
| --- | --- |
| Binder | PG 64-22 |
|  | Left | Right |
|  | ID | Air Void, % | ID | Air Void, % |
|  | MD 318.06 | 7.1 | MD 318.04 | 6.8 |
|  | MD 318.07 | 6.9 | MD 318.05 | 7.2 |
| Rut Depth at 7,000 passes, mm | 12.5 |  |
| Rut Depth at 4,600 passes, mm |  | 12.5 |
| Creep Slope, Passes/mm | 1,420 | 800 |
| Strip Slope, Passes/mm | 370 | 256 |
| Stripping Inflection Point | 3,850 | 2,800 |